LST-000232 Payload Forbidden And Restricted Materials List

TABLE OF CONTENTS

1	Table of Contents	3

2	Applicable Documents	4

3	Scope	5

4	Forbidden Materials	6

4.1	Stress Corrosion Cracking	10

4.2	Electronical Components	10

4.3	Outgassing	11

5	Restricted Materials	12

5.1	Stress Corrosion Cracking: restricted material	15

# Table of Contents

  - Table of Contents

  - Applicable Documents

  - Scope

  - Forbidden Materials

    - Stress Corrosion Cracking

    - Electronical Components

    - Outgassing

  - Restricted Materials

    - Stress Corrosion Cracking: restricted material

# Applicable Documents

| AD# | Title | Doc No. |
| --- | --- | --- |
| AD-1 | ECSS: Space PA - Materials, mechanical parts and processes | ECSS-Q-ST-70C Rev.2 |
| AD-2 | ECSS: Space PA - Materials, processes and their data selection | ECSS-Q-ST-70-71C Rev.1 |
| AD-3 | ECSS: Space PA - Qualification and procurement of printed circuit boards | ECSS-Q-ST-70-60C |
| AD-4 | ECSS: Space PA - High reliability assembly for surface mount and through hole connections | ECSS-Q-ST-70-61C |
| AD-5 | ECSS: Space PA - Preparation, assembly and mounting of RF coaxial cables | ECSS-Q-ST-70-18C |
| AD-6 | ECSS: Space Engineering - Fracture control | ECSS-E-ST-32-01C |
| AD-7 | RIDESHARE PAYLOAD USER’S GUIDE (from SpaceX) | RPUG |

# Scope

This document shall be considered applicable for any payload requiring IOD/IOV services in the framework of ASI IOD/IOV initiative.

The list of materials is divided into Forbidden and Restricted.

Inside each category the material interested by the limitiation is presented together with the cause of such limitation, when available, and the reference source in ECSS or other standards.

# Forbidden Materials

The materials presented in Table 1 shall not be used for any space application. For Ground Support Equipments (GSE), Table 1 shall apply as follows:

  - for GSE undergoing vacuum activities all materials shall be considered forbidden,

  - for GSE not undergoing vacuum activities only materials involving causes of Toxicity, Fracture risk and Off-gassing shall be considered forbidden.

Every forbidden material shall not be considered neither for the design nor for COTS.

| Table 1: List of prohibited materials |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Forbidden material | Category | Description | Cause | Source | ID |
| Tin (pure, more than 97%) | Metal | Pure (or more than 97% alloys) metal used in coatings (obtained either by electroplating or hot- dipping) or connections: prohibited due to tin whiskers formation that may cause shortcircuits. | Tin wiskers and shortcircuiting | ECSS-Q- ST-70C | ECSS-Q-ST-70_0490061 |
| Mercury (pure and its compounds) | Metal | Liquid metal or used in compound form: prohibited due to high toxicity and volatility. | Toxicity, Volatility | ECSS-Q- ST-70C | ECSS-Q-ST-70_0490242 |
| Cadmium | Metal, Surface treatment | Metal alloy, also used in coatings and surface treatments: prohibited due to toxicity and vacuum sublimation. | Sublimation in vacuum | ECSS-Q- ST-70C | ECSS-Q-ST-70_0490239 |

| Table 1: List of prohibited materials |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Forbidden material | Category | Description | Cause | Source | ID |
| Beryllium and beryllium oxide | Metal | Metallic or ceramic element: prohibited due to toxicity of the pure form and its compounds. | Toxicity | ECSS-Q- ST-70C | ECSS-Q-ST-70_0490242, ECSS-Q-ST-70_0490243 |
| Zinc | Metal, Surface treatment | Metallic form or used as surface treatment: prohibited due to sublimation in vacuum. | Sublimation in vacuum | ECSS-Q- ST-70C | ECSS-Q-ST-70_0490239 |
| Titanium alloy (fasteners) for safe life applications | Metal | Titanium alloy fasteners: prohibited for safety- critical applications due to fracture risk. | Fracture risk | ECSS-E- ST_32-01 | ECSS-E-ST_32-01_0810187 |
| Hexavalent chromium surface treatments (Alodine 1200s, Chromic anodizing etc) | Surface treatment | Surface treatment (e.g., Alodine 1200, chromic anodizing): prohibited due to toxicity under REACH regulations. | Toxicity | REACH Regulati ons | - |
| Chlorinated materials | Polymer, Solvent, Flame retardant | Chlorinated solvents or flame retardants: prohibited due to outgassing and corrosive by- products. | Outgassing, Corrosive by- products | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260105 |

| Table 1: List of prohibited materials |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Forbidden material | Category | Description | Cause | Source | ID |
| Polyvinyl Chloride (PVC) | Polymer (Tape) | Polymer used in tapes or sleeves: prohibited due to outgassing in space environments. | Outgassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260063 |
| Cellulose | Polymer (Thermoplastics) | Thermoplastic polymer used in films or foams form: prohibited due to outgassing behavior. | Outgassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260127 |
| Acetates | Polymer (Thermoplastics) | Thermoplastic polymer used in films or foams form: prohibited due to outgassing behavior. | Outgassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260127 |
| Polyvinyl Acetate | Polymer (Thermoplastics) | Polymeric adhesive or coating: prohibited due to outgassing behavior. | Outgassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260129 |
| Polyvinyl Butyrate | Polymer (Thermoplastics) | Adhesive film or binder: prohibited due to outgassing behavior. | Outgassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260130 |
| Fluorocarbon (sleeves) | Polymer (Fluoropolymer) | Fluorocarbon sleeve insulators: prohibited due to outgassing behavior and low radiation resistance. | Outgassing, Degradation | ECSS-Q- ST-70-61 | ECSS-Q-ST-70-61_1510469 |

| Table 1: List of prohibited materials |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Forbidden material | Category | Description | Cause | Source | ID |
| Polyester (pure and in composites containing styrene) | Polymer (Resin) | Polymer in resin form or used as styrene-based composite: prohibited due to toxicity, volatility, and incompatibility with PCBs. | Toxicity, Volatility, Detrimental for PCBs | ECSS-Q- ST-70-71 | ECSS-Q- ST-70-71_1260137, ECSS- Q-ST-70-71_1260098 |
| Alkyd-type coatings | Coating | Protective alkyd-based paint: prohibited due to emission of volatile organic compounds at room temperature. | Off-gassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260057 |
| Polyester-type coatings | Coating | Polyester-based coating: prohibited due to off- gassing at room temperature. | Off-gassing | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260057 |
| Polysulphide-type coatings | Coating, Potting, Elastomer | Elastomeric sealant or coating: prohibited due to off-gassing at room temperature. | Off-gassing | ECSS-Q- ST-70-71 | ECSS-Q- ST-70-71_1260086, ECSS- Q-ST-70-71_1260104 |
| Graphite (Pure) | Lubricant | Dry lubricant in powder or film: prohibited due to abrasiveness in vacuum environment. | Abrasive under vacuum | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260083 |

| Table 1: List of prohibited materials |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Forbidden material | Category | Description | Cause | Source | ID |
| Asbestos | Non-Metal | Non-metallic insulating fiber: prohibited due to high toxicity and carcinogenic risk. | Toxicity | ECSS-Q- ST-70-71 | ECSS-Q-ST-70-71_1260146 |

## Stress Corrosion Cracking

The use of alloys provided in ECSS-Q-ST-70-36C Table 5-3 are forbidden due to low resistance to SCC.

## Electronical Components

ECSS-Q-ST-60C provide details for EEE material selection (ECSS-Q-ST-60_0480031). For a better accessibility, the requirements are reported below.

These materials are prohibited because their usage affects Safety or Launch Provider Guidelines:

    - Hollow core resistors

    - Potentiometers

    - Non-metallurgically bonded diodes

    - Semiconductor dice with unglassivated active area

    - Wet slug tantalum capacitors other than capacitor construction using double seals and a tantalum case

    - Aluminium liquid electrolytic capacitors

    - Tin coated wires and cables

    - PVC insulated wires and cables

## Outgassing

The criteria to define the selection of a material accounting its outgassing behavior are expressed in terms of:

- TML % (Total Mass Loss);

- CVCM % (Collected Volatiles);

- RML % (Recovered Mass Loss);

- WVR % (Water Vapor Recovered).

Each individual non-metallic material used in flight hardware or ground hardware that will be exposed to vacuum shall satisfy the criteria for Recovered Mass Loss (RML) and Collected Volatile Condensable Material (CVCM) reported in Table 2, when tested per ASTM E-595 or ECSS-Q-ST-70-02.

| Table 2: Outgassing requirements for materials |  |  |  |
| --- | --- | --- | --- |
| RML | CVCM | Additional Criteria | Source |
| < 1% | < 0,1% | None, always compliant | ECSS-Q-ST-70-02_0510082 , RPUG |
| < 3% | < 0,1% | Exposed area < 2 in2 | RPUG |
| > 3% | > 0,1% | Exposed area < 0,25 in2 | RPUG |

Nevertheless, in case of more relaxed criteria (second and third rows of the table), the location of the outgassing material shall ensure a null view factor towards identified Sensitive Items surfaces.

# Restricted Materials

The restricted materials reported in this section are usually treated by D-Orbit as limited to cases where the material usage is necessary because no alternatives are available.

In the framework of ASI IOD/IOV Program, any potential utilization by payload owner of the materials reported in this section shall be justified by the payload owner and approved by D-Orbit.

Every restricted material shall also be considered in the Hazard Analysis of the Program and the Go/No Go will be the Hazard Analysis output.

When possible, the following table provide the causes and the limitations for the usage of the restricted materials in terms of operative conditions, coupling or processes. The reference to ECSS is also indicated and the user is invited to check them to understand the context of the specifications.

| Restricted Materials | Detail, Rationale | Cause | ECSS Reference |
| --- | --- | --- | --- |
| Nickel (pure, high Ni alloys) | when in contact with Sulphur | Embrittlement | ECSS-Q-ST-70-71_1260011 |
| Unstabilized austenitic (Stainless) Steel | shall not be used at temperatures above 370 °C |  | ECSS-Q-ST-70-71_1260021 |
| 400-series stainless steels | shall guarantee risk control to | Embrittlement, corrosion, SCC | ECSS-Q-ST-70-71_1260022 |
| Magnesium alloy | shall demonstrate protection to | Corrosion, Flammability | ECSS-Q-ST-70-71_1260034 ECSS-Q-ST-70-71_1260035 |

| Restricted Materials | Detail, Rationale | Cause | ECSS Reference |
| --- | --- | --- | --- |
| Beryllium alloys and Beryllium-oxide | shall not be used if content of Be > 4% by weight |  | ECSS-Q-ST-70-71_1260037 |
| Copper coatings | shall not be used on external surfaces of space systems exposed to atomic oxygen in LEO | Atomic Oxigen effects | ECSS-Q-ST-70-71_1260009 |
| Silver coatings | shall not be used on external surfaces of space systems exposed to atomic oxygen in LEO | Atomic Oxigen effects | ECSS-Q-ST-70-71_1260040 |
| Osmium coatings | shall not be used on external surfaces of space systems exposed to atomic oxygen in LEO | Atomic Oxigen effects | ECSS-Q-ST-70-71_1260041 |
| Aluminium wrought alloy 5456, 5083, 5086 | shell be used only in controlled tempers (H111, H112, H116, H117, H323, H343) | SCC, exfoliation | ECSS-Q-ST-70-71_1260004 |

| Restricted Materials | Detail, Rationale | Cause | ECSS Reference |
| --- | --- | --- | --- |
| Silicone materials | shall not be used in pressurized systems requiring low gas permeability |  | ECSS-Q-ST-70-71_1260106 |
| Lead finishes | shall have minimum 3 % Lead in case of tin/lead finish |  | ECSS-Q-ST-70-61_1510136 |
| Pink-polyethilene (bags, film, bubble wrap or foam) | shall not be used near any ESD-sensitive item or within an ESD protected area | ESD | ECSS-Q-ST-70-61_1510043 |
| Polystyrene (foam) | shall not be used near ESD- sensitive items unless shielding overwrap protects them |  | ECSS-Q-ST-70-61_1510044 |
| Tin-Lead assemblies | shall not be used on gold plated pads |  | ECSS-Q-ST-70-08, 6.8.2 a |
| Molybdenum and Copper-Infused-Ceramics | shall not be used in RF PCBs |  | ECSS-Q-ST-70-12, 12.2 e |

Additionally, usage of carginogens, radioactive, friable and (hard and soft) magnetic material shall be subjected to justification.

## Stress Corrosion Cracking: restricted material

From ECSS-Q-ST-70-36C, Section 5.2.3 provide alloys (steel, aluminium, copper, magnesium) with moderate resistance to stress corrosion cracking (SCC). D-Orbit shall consider the materials presented there as restricted materials. Any potential utilization of these materials shall be justified.